## Slide 1
SATURN DOE Report
[DP Process]
2026.09.12
김용모

## Slide 2
Purpose
Results
SATURN 제품의 양산성 검증을 위해 DP 공정(Lamination, Back Grind, Saw)의 표준 작업 조건 및 품질 특성(CTQ)의 공정 능력(Cpk)을 최종 검증함
Conclusion
2차 DOE 치핑 불량에 대한 원인 분석 및 개선 대책 수립을 완료하여 3차 DOE에서 안정적인 품질을 확보함. DP 전 단위 공정의 CTQ 규격을 만족하였으므로 양산화 검증(Mass Qual) 진행을 승인
Step | Machine | Raw Material (각 단위 공정에서 선정한 BOM) | Test Item (단위 공정의 주요 평가항목/CTQ) | Result
SMT | HYBRID5 | WS693CPS (Alphametal) 0603 Resistor dummy (MURATA) 0402 Capacitor dummy (MURATA) | VISUAL, Capacitor Shear Test | PASS / Fail
Lamination | RU-3520 | BG Tape: E-6142S (LINTEC) | VISUAL, TAPE VOID | PASS / Fail
Back Grind | DGP8761 | Rough/Fine Wheel, DAF: FH-7221S(T) | WAFER THICKNESS, ROUGHNESS, TTV | PASS / Fail
Wafer Saw | DFD6361 | Blade: ZH05-SD3500-N1-50-CE / FD | KERF WIDTH, CHIPPING, CRACK | PASS / Fail
DA |  |  |  | 
WB |  |  |  | 
MD |  |  |  | 
BE |  |  |  | 
SATURN Project _ DOE Report
1st DOE(Done)
2nd DOE(Done)
3rd DOE(Done)

## Slide 3
Package / Wafer Information
PCB Description
PKG Type | Project Code | Wafer Size(inch) | Die Size(mm) | Target Thickness(um) | Scribe Lane(㎛) | DAF Thickness(um)
BGA | SATURN | 12 | 9.916 x 2.080 | 250 | 80 | 20
PCB / Substrate |  |  | 
Spec. No. | Part No. | Core | SR
ADS******* | APF****** | ***** | *****
SATURN Project _ DOE Report

## Slide 4
Saw
2nd Inspection
Post Cure
UV Exposure
Die Attach
Mold
Plasma
Lamination
Back-grind
Wafer incoming
FVI
Shipping
Marking
3rd Inspection
Cure
Plasma Clean
Wire Bonding
Bake
Strip Test
SMT Bake
(Sub Bake)
SMT_Front
SMT_Deflux
PCB incoming
Process Flow
SATURN Project _ DOE Report
DP

## Slide 5
품질 검사 검토 항목 (CTQ Check)
Process | Inspection Item | Sample Size
BG Tape LAMINATION | VISUAL | 1 SUB / M.C / 1st LOT
Wafer BACK GRIND | WAFER THICKNESS | 13 Points / All Wafer
 | WAFER ROUGHNESS | 5 Points / Each Wafer
 | WAFER TTV | 12inch
Wafer Saw | KERF WIDTH | 10 Points / All Wafer (또는 10Points / Each Wafer)
 | CHIPPING / CRACK | All Wafer / Run (또는 2 Wafer / Each Evaluation)
PCB SMT | VISUAL | 1SUB /M.C/1st LOT
DIE ATTACH | VISUAL | 1 SUB/M.C/1st LOT
 | TAPE VOID | 2 UNIT/M.C/1st LOT
 | DIE ACCURACY | 20 UNIT/M.C/1st LOT
 | BONDLINE THICKNESS | 20 UNIT/M.C/1st LOT
 | PARAMETER | M.C/ 1st LOT
Process | Inspection Item | Sample Size
WIRE BONDING | VISUAL/PARA | 1 SUB/M.C/1st LOT
 | BOND PULL TEST(*) | 55 WIRE/M.C/1st LOT
 | BALL SHEAR TEST(*) | 22 BALL/M.C/1st LOT
 | LOOP HEIGHT | 11 WIRE/M.C/1st LOT
 | BALL HEIGHT | 11 WIRE/M.C/1st LOT
 | BALL DIAMETER | 11 WIRE/M.C/1st LOT
 | KOH ETCHING | 5WIRE/M.C/ 3 LOTS
IVI GATE | VISUAL | AQL 0.065%/LOT
MOLDING | VISUAL/PARA | 1 SHOT/M.C/1st LOT
 | S.A.T | 1 SHOT/M.C/1st LOT
 | X-RAY | 1 SHOT/M.C/1st LOT
 | Mold Thickness check | 1 STRIP /1st LOT
MARKING | VISUAL | 1SUB /M.C/1st LOT
SATURN Project _ DOE Report
★ HINT ★
초기 제품 개발 검토 단계에서 수립된 검사 항목 및 샘플링 검사 수량을 기입한다.
어떤 목적으로 검토되었던 내용인지 명확히 알고 있어야 하며, 6Page 부터는 검사된 결과가 Data로 명시되어 고객에게 품질 특이사항이 없음을 보여주는 근거 자료로 활용된다.

## Slide 6
1. Back Grind Process Condition & Result
2) Visual Inspection Result (9Page 참조 / Visual 결과는 특이사항 없는 것으로 함)
Item | Lot No. | Sample Size | Inspection Results | 
Visual Inspection | DOE Lot | 2 wafer / each evaluation | Pass / Fail | 2 wafer / each evaluation
Item | Spec | Applied Condition
Mount Table temp (°C) | 75 ± 5 | 75 (또는 75 ℃)
Wheel RPM (RPM) | G1 : 2700±500 / G2 : 2700±500 | G1 : 2700 / G2 : 2700
Wheel Feed (um/sec) | G1 : 6±4 / 5±3 / 4±3 G2 : 0.7±0.3 / 0.4±0.3 / 0.4±0.3 | G1 : 5.0 / G2 : 0.5
Chuck Speed (RPM) | G1 : 300 / 300 / 300 G2 : -300 / -300 / -300 | G1 : 300 / G2 : -300
3) Wafer Roughness
1) Process Condition
Lot No. | Spec | Sample Size | Test Step | Result | Data (nm) |  |  |  |  | Min. | Max. | Avg. | Std. | Cpk.
DOE Lot | Polishing Skip ≤ 200nm | 5Points / Each Wafer | 1차_1st wf | Pass/Fail | 76.47 | 87.37 | 84.49 | 85.24 | 76.47 | 76.47 | 87.37 | 83.03 | 4.56 | 8.54
 |  |  | 1차_2nd wf | Pass/Fail | 72.51 | 74.72 | 76.54 | 77.96 | 70.37 | 72.51 | 77.72 | 74.42 | 4.01 | 20.51
 |  |  | 2차_1st wf | Pass/Fail | 73.80 | 82.70 | 77.34 | 71.60 | 66.52 | 66.52 | 82.70 | 74.39 | 2.04 | 8.68
 |  |  | 2차_2nd wf | Pass/Fail | 75.06 | 83.20 | 74.09 | 72.53 | 83.75 | 72.53 | 83.75 | 80.44 | 4.29 | 3.29
 |  |  | 3차_1st wf | Pass/Fail | 74.70 | 74.70 | 74.76 | 76.57 | 73.01 | 73.01 | 76.57 | 79.18 | 2.45 | 10.05
 |  |  | 3차_2nd wf | Pass/Fail | 72.70 | 70.29 | 74.42 | 74.42 | 81.38 | 70.29 | 81.38 | 76.31 | 1.71 | 17.62
※ Raw Data (참고)
SATURN Project _ DOE Report

## Slide 7
4) Wafer Thickness
Lot No | Spec | Sample Size | Test Step | Result | Data |  |  |  |  |  |  |  |  |  |  |  |  | Min. | Max. | Avg. | Std. | Cpk.
DOE Lot | 250±10um (Target : 250um) | 13Points/ Each Wafer | 1차_1st wf | Pass | 249.1 | 252.2 | 249.5 | 251.6 | 248.7 | 250.2 | 248.6 | 249.3 | 252.8 | 250 | 250.5 | 248.6 | 252.9 | 248.6 | 252.9 | 250.36 | 1.52 | 2.11
 |  |  | 1차_2nd wf | Pass | 249.6 | 250.4 | 251.1 | 249.8 | 251.3 | 251.8 | 251.6 | 249.2 | 250 | 249.5 | 249.1 | 251.1 | 249.9 | 248.3 | 251.4 | 250.58 | 0.9 | 2.81
 |  |  | 2차_1st wf | Pass | 249.4 | 249.4 | 252.1 | 251.6 | 250.1 | 250.7 | 250.1 | 249.3 | 249.1 | 250.8 | 249.1 | 249.2 | 248.6 | 242.5 | 250.9 | 250.38 | 1.12 | 3.23
 |  |  | 2차_2nd wf | Pass | 252 | 250.1 | 250.8 | 250.3 | 251.1 | 249.4 | 250 | 249.6 | 252.2 | 250.5 | 250.3 | 249.7 | 249.4 | 249.3 | 252 | 249.87 | 0.49 | 6.66
 |  |  | 3차_1st wf | Pass | 251.3 | 249.2 | 250.7 | 249.8 | 250.5 | 250.7 | 250.4 | 250.4 | 250.1 | 251.5 | 251.8 | 248 | 251.4 | 248 | 252.2 | 250.62 | 0.76 | 4.13
 |  |  | 3차_2nd wf | Pass | 249.7 | 250 | 251.1 | 251.9 | 253 | 251.5 | 251.3 | 250.9 | 250.3 | 249.7 | 251.5 | 253 | 250 | 249.7 | 253 | 251.1 | 1.1 | 1.7
5) Wafer TTV (Total Thickness Variation) – Wafer 1매의 두께 오차(평탄도)
Lot No | Spec | Test Step | Inspection Results | 
DOE Lot | 12inch : [ Max-Min ] ≤ 10um | 1차_1st wf | Pass | 4.3 um
 |  | 1차_2nd wf | Pass | 3.1 um
 |  | 2차_1st wf | Pass | 8.4 um
 |  | 2차_2nd wf | Pass | 2.7 um
 |  | 3차_1st wf | Pass | 4.2 um
 |  | 3차_2nd wf | Pass | 3.3 um
1. Back Grind Process Condition & Result
SATURN Project _ DOE Report

## Slide 8
2) Visual Inspection Result (9Page 참조 / Visual 결과는 특이사항 없는 것으로 함)
Item | Lot No | Sample Size | Inspection Results | 
Visual Inspection | DOE Lot | 2 wafer / each evaluation | Pass / Fail | 2 wafer / each evaluation
Item | Spec | Applied Condition | Remark
Cut Method | Wafer 특성에 따름 | Step Cut | 
Blade Model | Wafer 특성에 따름 | Z1 : SD3500-N1-50-CE Z2 : SD3500-N1-50-FD | 
Cut Speed (Step Cut) | Max 80mm/sec | 60 mm/sec | 규격 만족
Spindle RPM | 30000~55000 RPM | Z1 : 50,000 / Z2 : 40,000 RPM | 규격 만족
Blade Height (Z1 / Z2) | Wafer + Mount Tape 특성에 따름 | Z1 : 0.240 mm / Z2 : 0.080 mm | 
1) Process Condition
2. Saw Process Condition & Result
3) Kerf Width
Lot No | Spec | Sample Size | Test Step | Result | Data |  |  |  |  |  |  |  |  |  | Min. | Max. | Avg. | Std. | Cpk.
DOE Lot | Max 65um | 10Points/ Each Wafer | 1차_1st wf | Pass/Fail | 64.9 | 63.3 | 62.3 | 61.8 | 63.5 | 60.5 | 59.8 | 60.5 | 64.3 | 62.5 | 59.8 | 64.9 | 62.34 | 1.71 | 0.52
 |  |  | 1차_2nd wf | Pass/Fail | 60.2 | 60.9 | 60.4 | 60.1 | 60.9 | 63.3 | 59.4 | 59.3 | 64.3 | 61.6 | 59.3 | 64.3 | 61.04 | 1.61 | 0.81
 |  |  | 2차_1st wf | Pass/Fail | 59.8 | 59.2 | 62.7 | 62.4 | 59.4 | 60.4 | 63.9 | 63.8 | 62.3 | 59.5 | 59.2 | 63.8 | 61.34 | 1.87 | 0.65
 |  |  | 2차_2nd wf | Pass/Fail | 61.2 | 60.5 | 60.8 | 59.5 | 61.5 | 60.1 | 59.5 | 62.3 | 62.8 | 63.6 | 59.5 | 63.6 | 61.18 | 1.38 | 0.92
 |  |  | 3차_1st wf | Pass/Fail | 63 | 60.6 | 59.8 | 62.3 | 62.5 | 60 | 59.9 | 62.5 | 61.1 | 61 | 59.8 | 63 | 61.27 | 1.21 | 1.02
 |  |  | 3차_2nd wf | Pass/Fail | 60.3 | 64.2 | 63.4 | 61.1 | 60.9 | 64.6 | 61.3 | 61.7 | 61.8 | 59 | 59 | 64.6 | 61.83 | 1.76 | 0.6
SATURN Project _ DOE Report

## Slide 9
Sample | Result | Top Image | Side Image
1St | Pass |  | 
2nd | Pass |  | 
3rd | Pass |  | 
5) Image
3. Saw Process Result
-. There is no top or back side chipping, lateral crack. Sawing condition is all ok.
Pattern Side
Pattern Side
Pattern Side
SATURN Project _ DOE Report

## Slide 10
앞에서 작성하신 DOE Report 를 자세히 훑어보고 멘토가 제공하여 드린 Data 중 Engineer Evaluation 결과로 적합하지 않은 부분을 찾고 그 이유를 기술해 주세요.
※ 주어진 상황 중 오류 발견하기
첫번째 발견된 문제점 : Back Grind 두께 데이터 중 2차_1st Wafer의 2번 측정 포인트 값이 222um로 기재
부적합 이유
SATURN 웨이퍼 두께 Spec은 250 ± 10 um (240 ~ 260 um)이므로, 222 um는 규격 하한을 크게 벗어난 심각한 Spec-out(불량)임.
그러나 동일 열의 최소값(Min)에는 242.5 um로 잘못 기재되어 있고 판정도 'Pass' 처리되어 있음.
이는 장비 헌팅 에러 또는 단순 오기입(242.x um 오타)으로 보이며, 이상치를 확인/재측정하지 않고 그대로 통계 처리하여 'Pass' 낸 것은 엔지니어링 데이터로 부적합함.
두 번째 발견된 문제점 : Saw 공정 Kerf Width 결과가 1~3차 모두 'Pass'로 판정되어 있으나, 산출된 공정능력지수(Cpk)는 0.52 ~ 1.02에 불과함.
부적합 이유
1. 반도체 양산 승인(Mass Qual) 기준 최소 요구 Cpk는 통상 1.33 이상 (우수 공정은 1.67 이상)임.
2. 실측치 자체는 상한 규격(Max 65 um) 미만이나, 평균값(61~62 um)이 상한 규격에 너무 근접하여 공정 마진이 매우 부족함.
3. 따라서 Cpk 기준(1.33)을 미달함에도 단순 실측 수치가 규격 내에 있다는 이유로 'Pass' 판정하여 양산으로 넘기는 것은 엔지니어 평가 결과로 적합하지 않음.